## SLAC Traveler for HXR Undulator #29H929-022 in MMF

Dataset 001

This traveler is intended to cover preparation, magnetic measurements, and fiducialization of the HXR undulator segments at MMF.

Preparation:

- Remove all protective covers.

- Remove plastic cover. Clean up the granite.

- Label modules from 1 to 3.

- Remove the motor covers on the bench side.

| Vendor serial number from undulator label: |  |
| --- | --- |
| Technician (initials): |  |
| Date/Time: |  |

- Call controls group to hook-up and check the control system. Check completed.

- Call alignment crew to align the undulator to the bench. Alignment done.

- Open gap to 100mm. Attach temperature sensors. Reset the load cells.

- Install brackets for the vacuum chamber limit switches.

- Turn ON the bench. Manually move the carriage to check for interferences.

- Initialize the bench.

Tuning.

Follow the check list below, consult with the tuning test plan (LCLS-TN-17-1).

Tuning process checklist:

| Engineer (initials): |  |
| --- | --- |
| Tuning started, Date (mm-dd-yyyy): |  |
| Undulator magnetically aligned at tuning Gap = 9mm (check load cells’ readings, balance cells in necessary); results recorded in the table below. |
| Find magnetic center at min B, record X position in the table. |
| Match half-gap and full-gap encoder readings at 9.0 mm gap |
| Upstream RM measured |
| Kugler bench OFF, Long coil set, PDI and XPS ON |
| Field integrals measured for tuning trajectories |
| Coil and stages in park position, PDI and XPS OFF, the coil removed for shimming. |
| Shim table prepared. Gap opened to 100mm. |
| Undulator trajectory shimming completed |
| Kugler bench ON and re-initialized |
| Trajectories and phase errors checked. (If additional shimming needed, repeat Hall probe measurements, coil measurements and tuning). |
| Trajectories and phase errors tuned to tolerances. |
| Fields measured for tuning ends. |
| Kugler bench OFF. Long coil set, PDI and XPS ON |
| Field integrals measured for tuning first and second field integrals. |
| Shim table prepared. Gap opened to 100mm. The coil removed for shimming. |
| Field integrals tuning done. |
| Long coil set back, PDI and XPS ON. |
| Undulator field integrals checked. If additional shimming needed, repeat coil measurements and tuning. |
| Field integrals shimming completed. |
| Field integrals measured for finding commissioning gap. |
| Coil and stages set in park position, PDI and XPS OFF, the coil removed. shimming. |
| Kugler bench ON and re-initialized. |
| MA position vs X checked. |
| Trajectories and phase errors checked and within the tolerances. |
| Hall probe measurements to find commissioning gap done. |
| Phase matching done. |
| Coil installed; optical measurement of coil position done. |
| Field integrals vs gap checked. |
| Final scan done, coil |
| Coil and stages set in park position. PDI and XPS OFF, the coil removed. |
| Gap clearance checked. Gap =7.350mm |
| Voltmeters checked. |
| Kugler bench ON and re-initialized. |
| Reference magnet measured. |
| MA position vs X checked. Gap = 9mm |
| Capacitive sensor measurements, gap = 7.5 mm |
| Final scan done, Hall probe. |
| PMs attached. |
| PMs measured for fiducialization, file with results created. |
| Fiducialization done. |
| Capacitive sensor measurements, poles #10, 20, 240, 250 done. |
| Controller Configuration saved. |

The following information is to be noted by an engineer:

| Feet Position (A, B, or C): | B |
| --- | --- |
| Closed loop Encoders | Full-Gap, Renishaw |
| Average X (m): |  |
| Average Y (m): |  |
| Final Pitch (µrad): |  |
| Final Yaw (µrad): |  |
| Magnetic axis position X (m): |  |
| Magnetic axis position Y (m): |  |
| Coil X-position (m) |  |
| Coil Y-position (m) |  |
| Commissioning Gap (mm) |  |
| Reference magnet measurement (T) |  |
| Voltmeter X (6V) 6.00007 |  |
| Voltmeter X (-6V) -6.00007 |  |
| Voltmeter X (1V) 1.00002 |  |
| Voltmeter Y (1V) 1.00002 |  |

Load cells’ readings at gap = 9.0 mm

| UWU upstream bench up |  |
| --- | --- |
| UWL upstream bench low |  |
| UAU upstream aisle up |  |
| UAL upstream aisle low |  |
| DWU downstream bench up |  |
| DWL downstream bench low |  |
| DAU downstream aisle up |  |
| DAL downstream aisle low |  |

Fiducialization:

The following information is to be noted by an engineer:

| Engineer (Initials): |  |
| --- | --- |
| Upstream RM X offset (m): |  |
| Upstream RM Y offset (m): |  |
| Downstream RM X offset (m): |  |
| Downstream RM Y offset (m): |  |
| Upstream PM X offset (m): |  |
| Upstream PM Y offset (m): |  |
| Downstream PM X offset (m): |  |
| Downstream PM Y offset (m): |  |

Have an alignment crew to measure offsets between RM and the undulator fiducials.

| Surveyor (initials): |  |
| --- | --- |
| Date (mm/dd/yyyy): |  |

Prepare the undulator for the move into the storage area:

- Power OFF the controller. Disconnect the network cable.

- Remove vacuum chamber limit switch brackets.

- Remove temperature sensors.

- Remove long coil brackets.

- Install all protective covers.

- The undulator is ready for move into the storage area.

| Technician (initials) / date: |  |
| --- | --- |

URL for data:

V:\MET\MagServe\MagData\LCLS-II\Undulator\HXU_022 \DATASET0001 \Final Results\

| Undulator tuning completed (signed): |  |
| --- | --- |