## SLAC Traveler for SXU reference undulator check.

## Dataset 0012

Placing undulator on the measurement bench:

| Earthquake T-bolts checked |  |  |
| --- | --- | --- |
| Thermistor blocks attached |  |  |
| Check interference with probes |  |  |
| Technician (initials): |  |  |
| Date (mm-dd-yyyy): |  |

Tuning.

Follow the fine tuning test plan to align the undulator to the bench, measure x , y field and calculate the trajectories, phases and field integrals, and fiducialize the undulator (LCLS-TN-06-17, LCLS-TN-07-2). X and Y to be set to 10µm; roll to 0.1mrad; pitch to 0.005mrad, and yaw to 0.010mrad.

| Mechanical alignment done |  |
| --- | --- |
| Capacitive sensor measurements done |  |
| Probe roll angle checked |  |
| Magnetic alignment done |  |

The following information is to be noted by an engineer upon finishing alignment to the granite:

| Engineer (initials): |  |
| --- | --- |
| Date (mm-dd-yyyy): |  |
| First pole position(m) |  |
| Final Roll (µrad): |  |
| Average X (m): |  |
| Average Y (m): |  |
| Final Pitch (µrad): |  |
| Final Yaw (µrad): |  |

Measurement process checklist:

| X0, Y0 at nominal K found and recorded |  |
| --- | --- |
| Trajectories, phases, and K checked |  |
| Upstream PM measured |  |
| Kugler bench OFF |  |
| Long coil set for final measurements |  |
| Optical measurement of coil position done |  |
| Field integrals checked |  |
| Coil and stages in park position |  |
| Kugler bench ON and re-initialized |  |
| Reference magnet measured |  |
| Voltmeters checked w.r.t. voltage standard |  |
| Final Measurement done |  |

The following information is to be noted by an engineer upon final tuning:

| Engineer (Initials): |  |
| --- | --- |
| Date (mm/dd/yyyy) |  |
| Reference magnet measurement (T): |  |
| First integral Y at center (µTm): |  |
| Second integral Y at center (µTm2): |  |
| First integral X at center (µTm): |  |
| Second integral X at center (µTm2): |  |
| Magnetic axis position X (m): |  |
| Magnetic axis position Y (m): |  |
| Voltmeter X read (1V) 1.00002 |  |
| Voltmeter Y read (1V) 1.00002 |  |
| Voltmeter Y read (6V) 6.00007 |  |
| Voltmeter Y read (-6V) -6.00007 |  |
| Final Phase error rms ( ˚ ): |  |
| Undulator Temperature (˚C) |  |
| Measured K-value: |  |
| Upstream PM X-Offset (m): |  |
| Upstream PM Y-Offset (m): |  |
| Coil x-center |  |
| Coil y-center |  |