**APPLE-II short coil measurement results**

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Gap** | **I1y(µG·cm)** | **I2Y(µG·cm2)** | **I1X(µG·cm)** | **I2X(µG·cm2)** | **Comments** |
| 25mm | -462±16 | -717±34 | -241±33 | -498±74 |  |
| 14mm | -306±22 | -497±57 | -108±36 | +501±66 |  |
| 35.6 mm |  |  |  |  |  |
|  |  |  |  |  |  |
|  |  |  |  |  |  |

\* 7 measurements used for average and RMS calculations. Accuracy of first integral measurements is 30µG·cm; and 70µG·cm2for second field integral.