# MFD NON-COMPLIANCE REPORT # 4478

Date: 2/24/03

Job #: 16989

Sub ID:

Part Number: PF-293-121-92

Part Description: Rectangular to Rectangular Cover

Engineer: C. Rago

Ext: x3636

Reason For Non-compliance:

- Radius .016” is small by -.0063, Actual is .0087”

- Profile |.001|A|B| are out of tolerance as follows:

SN 002 is out by .0001”

SN 003 is out by .0004”

SN 004 is out by .0015”

SN 004 is out by .00035”

SN 005 is out by .0003”

SN 006 is out by .0003”

SN 007 is out by .00015

SN 008 is out by .0001”

SN 009 is out by .00015”

SN 010 is out by .00005”

SN 011 is out by .00015”

SN 012 is out by .0005”

SN 013 is out by .0001”

SN 014 is out by .00053”

SN 015 is out by .00035”

SN 016 is out by .0002”

SN 017 is out by .00015”

SN 018 is out by .0001”

SN 019 is out by .00015”

SN 020 is out by .00015”

1.  Check at dry fit braze and alter as necessary to fit flat

2.  Check at dry fit – remove any set that does not fit