# MFD NON-COMPLIANCE REPORT # 4483

Date: 2/27/03

Job #: 16876

Sub ID:

Part Number: PF-293-101-36 Rev. 0

Part Description: Splitter Assy. Base

Engineer: C. Rago

Ext: 3636

Reason For Non-compliance:

SN001:

- Basic dimension 1.442 unilaterally toleranced  (+.001/-.000) is  +0.0009” O.T. at the Top of base only (z = +1.300”)

SN002:

- Basic dimension 1.442 unilaterally toleranced  (+.001/-.000) is  -0.0001” O.T. at the Bottom of base only (z = +0.200”)

- Basic dimension 1.442 unilaterally toleranced  (+.001/-.000) is  +0.0002” O.T. at the Top of base only (z = +1.300”)

- Basic dimension 1.665 unilaterally toleranced  (+.001/-.000) is  -0.0005” O.T. (lid/cover distance)

See Inspection Report

Check 1.442 at braze assy.  Press to size.