# MFD NON-COMPLIANCE REPORT # 4484

Date: March 3, 2003

Job #: 16986

Sub ID:

Part Number: PF-290-309-38

Part Description: Jog Converter Machining WG Cover

Engineer: C. Rago

Ext: x3636

Reason For Non-compliance:

1.  Radius R.016” on all are undersized by .003”

2.  Flatness .002 is out on Serial Numbers:

SN 008 is over by  = .004”   .006” actual

SN 009 is over by  = .001”   .003” actual

- File lid to fit

- check at dry fit/ flatten or weight appropriately at braze.