# MFD NON-COMPLIANCE REPORT #5005

### Date:  3/31/03

Job #:  93-1243-5

Sub ID:

Part Number: PF-444-318-17 REV. 0

Part Description: BAR, FLUX SHIELD, K2

Engineer: D. ARNETT/J. LANGTON

Ext: 2070/2197

QTY: 2 PARTS

Reason For Non-compliance:

SN001 (ONLY):

- Distance 0.800” ± 0.005 (long slot side) measures 0.8395 (+0.0345” O.T.)

- Thickness 0.388” ± 0.002 measures 0.385 (-0.0010” O.T.)

BOTH PARTS:

- Perpendicularity of 0.001 (2X) ranges from 0.008” - .015”

Action Taken:

Anneal and straighten in house per D. Arnett.

Engineer Signature: __________________________ Date:______