# MFD NON-COMPLIANCE REPORT #5013

### Date:  5/7/03

Job #:  17323

Sub ID: 1

Part Number: SA-341-341-22 Rev. 1

Part Description:  Vacuum Side Flange

Engineer: L. Gianinni

Ext: 3143

QTY: 3

Reason For Non-compliance:

SN 02119-17:

- Flatness of depth plane 0.130 is .0023”

  - .130 is now .1455 (+.010” larger than pre-machining)

- Flatness of depth plane 0.046 is .0020

- Flatness of Knife edge is .0021”

  - Knife edge is not smooth on some edges

### SN 02119-18

- Flatness of depth plane 0.130 was .0019” now after machining is .0027”

- Flatness of depth plane 0.046 was .0018” now after machining is .0027

- Flatness of knife edge was .0009” now is .0021”

SN 20412-03

- All flatness’ (.130, .046, and knife edge) are .0012” - .0016”

Action Taken:

Engineer Signature: __________________________ Date:______