# MFD NON-COMPLIANCE REPORT # 5152

| PART NAME: | AIR SIDE STIFFNER | DATE: | 9/23/05 |
| --- | --- | --- | --- |
| PF/SA NO.: | PF-341-342-45 | INSPECTOR: | K. CABAN |
| WORK ORDER NO.: | 20294-35 | ENGINEER: | A. HILL | EXT.: | 4453 |
| VENDOR | MFD LIGHTMS | ROUTE TO: | VAC ASSY |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| Part Thickness 1.250 ± 0.005 is undersized 1.2400 (-0.005 under tolerance). On Part #2 only. Distance 21.695 ± 0.002 is undersized 21.6876 to 21.6893 (-0.0054 to -0.0037 under tolerance) on both parts. Distance 11.195 ± 0.002 is undersized 11.1885 (-0.0045 under tolerance) on Part #1 only. Distance 11.673 ± 0.002 is oversized 11.6788 to 11.6814 (+0.0038 to +0.0084 over tolerance) on both parts. |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |