# MFD NON-COMPLIANCE REPORT #5045

### Date:  1/15/03

Job #:  17704

Sub ID: -23

Part Number: PF-293-101-03 Rev. 01

Part Description:  Top Plate (Height Taper Assy)

Engineer: J. Chan

### Ext: 	5084

### QTY: 5

Reason For Non-compliance:

- |d|.001|A|B|C| is out of profile on SN002 only, undersized by approximately 0.0005”.  See Plot SN002.

- R .016 ± 0.001 is out of tolerance on all parts, ranging from 0.014” to 0.0182”.

  - Mating covers are all larger than the serialized base except for SN001.

Action Taken:

Engineer Signature: _____________________ Date:_________