# MFD NON-COMPLIANCE REPORT #5051

### Date:  1/30/04

Job #:  17597

Sub ID: -2

Part Number: SA-293-103-43 Rev. 0

Part Description:  Final Machining (Mode Stripper II)

Engineer: J. Chan

### Ext: 	5084

Reason For Non-compliance:

- 3X INDV. |d|.001|A|B|C| is out of surface profile on all three surfaces, see plots.

  - Engineer, noted that this condition was to be expected due to the deformation of the interior datum surfaces not being square and parallel.

- R 0.012 ± 0.001 measures 0.0095 – 0.0098 (undersized, but should be braze fit condition.

Action Taken:

Engineer Signature: _____________________ Date:_________