# MFD NON-COMPLIANCE REPORT # 5084

| PART NAME: | LOAD BODY | DATE: | 4/19/04 |
| --- | --- | --- | --- |
| PF/SA NO.: | PF-341-342-51 Rev. 2 | INSPECTOR: | K. Caban |
| WORK ORDER NO.: | 17784-42/30 | ENGINEER: | A. OWENS | EXT.: | 3168 |
| VENDOR | PACIFIC PRECISION MACHINE INC. | ROUTE TO: | PRECISION |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| ¦c¦.002¦ (x 0.030 SURFACE) IS OUT OF FLATNESS ON SN 01 ONLY BY 0.0009”. 13.874 ±0.005 IS UNDERSIZED BY 0.0014” SN 01 ONLY. 10.146 ±0.005 IS UNDERSIZED BY 0.0009” SN 01 ONLY. ¦j¦n.010m¦A¦Bm¦Cm¦ OF KEENSERTS ARE OUT OF POSITION ON HOLES MARKED IN RED ON BOTH PARTS BY A MAX OF 0.0450. 4 HOLES OUT OF 16 (2 PARTS). 9.500 +0.002/-0.000 IS UNDERSIZED BY 0.0015 SN 02 ONLY. | 1 2 3 4 5 |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |