# MFD NON-COMPLIANCE REPORT # 5105

| PART NAME: | TSP CHAMBER BASE WELDMENT MACHINING | DATE: | 7/2/04 |
| --- | --- | --- | --- |
| PF/SA NO.: | SA-342-410-13 R0 | INSPECTOR: | K. CABAN |
| WORK ORDER NO.: | 18322-26 | ENGINEER: | D. KHARAKH | EXT.: | 3215 |
| VENDOR | MFD LIGHTMS | ROUTE TO: | VAC. ASSY. |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| n 2.600 ± 0.005 IS OVERSIZED MEASURING 2.6316, (+0.0266” OUT OF TOLERANCE |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |