# MFD NON-COMPLIANCE REPORT # 5121

| PART NAME: | Cam Shaft 0.75MM Lift | DATE: | 1/6/05 |
| --- | --- | --- | --- |
| PF/SA NO.: | PF-380-705-11 REV. 1 | INSPECTOR: | T. Nakashima/K. Caban |
| WORK ORDER NO.: | 19494-3 | ENGINEER: | G. Bowden | EXT.: | 2991 |
| VENDOR | IMT | ROUTE TO: | LIGHTMS |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| ¦t¦.0002¦A¦B-C¦ OF n 1.1813 IS OUT OF TOTAL RUNOUT MEASURING 0.0010. n 1.1813 ±0.0002 MEASURES 1.1808 (TAPER EFFECT). ¦d¦.0010¦A¦F¦G¦ OF n .9845 IS OUT OF SURFACE PROFILE TO THE DATUMS A,F,&G SEE ATTACHED PROFILE PLOTS (RANGES FROM 0.012 TO 0.015). n .9845 ±0.0002 MEASURES 0.9849 (OVERSIZED BY 0.0001). ¦t¦.0002¦A¦F¦ OF n .7876 IS OUT OF TOTAL RUNOUT MEASURING 0.0022. n .7876 ±0.0002 MEASURES 0.7873. (UNDERSIZED BY 0.0001) |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |