# MFD NON-COMPLIANCE REPORT # 5136

| PART NAME: | WAVEGUIDE MA | DATE: | 8/8/05 |
| --- | --- | --- | --- |
| PF/SA NO.: | PF-380-605-02 REV 0 (REF PF-767-280-01 R3) | INSPECTOR: | K. CABAN |
| WORK ORDER NO.: | 20149-3 | ENGINEER: | J. CHAN | EXT.: | 5084 |
| VENDOR | MFD LIGHTMS | ROUTE TO: | PRECISION |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| ¦i¦.004¦H¦ of distance 1.662 is out of symmetry by 0.0103” on SN 3 ONLY. ¦i¦.004¦J¦ of distance 3.162 is out of symmetry by 0.0064” on SN 3 ONLY. Distance 3.488 ± 0.005 is out of tolerance 3.4795” (-0.0035 undersized out of tolerance) on SN 3 ONLY Distance 2.594 ± 0.005 is out of tolerance 2.5879” (-0.0011 undersized out of tolerance) on SN 5 ONLY. Distance 1.662 ± 0.001 is undersized by -0.0012 (1.6598) on SN 7 ONLY |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |