# MFD NON-COMPLIANCE REPORT # 5157

| PART NAME: | Cu FLANGE INSERT-ROT | DATE: | 10/20/05 |
| --- | --- | --- | --- |
| PF/SA NO.: | PF-293-142-45 | INSPECTOR: | K. CABAN |
| WORK ORDER NO.: | 20571-9 | ENGINEER: | C. RAGO | EXT.: | 3636 |
| VENDOR | MFD LIGHTMS | ROUTE TO: | PRECISION |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| 0.551 ± 0.001 measures 0.5480 (-0.0020 undersized out of tolerance) on SN 2 0.5488 (-0.0012 undersized out of tolerance) on SN 3 Surface Finish 125 max ranges from 125 – 150 on SN 2 & 3. Tool Line Marking around half of part on SN 3 only (See Picture) |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |