# MFD NON-COMPLIANCE REPORT # 5180

| PART NAME: | FLANGE MACHINING | DATE: | 4/6/06 |
| --- | --- | --- | --- |
| PF/SA NO.: | SA-380-805-08 | INSPECTOR: | K. Caban |
| WORK ORDER NO.: | 20438-2 | ENGINEER: | J. Chan | EXT.: | 5084 |
| VENDOR | MFD LIGHTMS | ROUTE TO: | PRECISION |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| SN 103 - has finger print marks on inner end. SN 102 - 5.202 ± 0.005 Measures 5.1959 ( -0.0011 undersized). SN 102 - ¦j¦.004¦C¦ is out of position by 0.0057 (+0.0017 out of position). |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |