# MFD NON-COMPLIANCE REPORT # 5185

| PART NAME: | VACUUM SIDE FLANGE | DATE: | 5/12/06 |
| --- | --- | --- | --- |
| PF/SA NO.: | SA-341-341-22 R2 | INSPECTOR: | K. CABAN |
| WORK ORDER NO.: | 20232-32 | ENGINEER: | A. HILL | EXT.: | 4453 |
| VENDOR | MFD LIGHTMS | ROUTE TO: | MTLFINSH |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| Surface finish of 16 measured 23 – 36.8 ra (see attached surf finish plot) Where helicoil holes were machined point sticks thru and was “sanded, polished or filed down. Note 8 on drawing specifies “Blend at intersecting surfaces smoothly”, on part, RESP. ENG please see if it is acceptable, edge kind of sharp R .125 ± 0.002 measures .130 - .131 R .063 ± 0.005 measures 0.053 |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |