# MFD NON-COMPLIANCE REPORT # 5199

| PART NAME: | CD1 CHAMBER HALF UPPER | DATE: | 7/28/06 |
| --- | --- | --- | --- |
| PF/SA NO.: | PF-451-060-11 R0 | INSPECTOR: | K. CABAN |
| WORK ORDER NO.: | 21651-1/50 | ENGINEER: | A. RINGWALL | EXT.: | 8508 |
| VENDOR | MFD LIGHTMS | ROUTE TO: | MTLFNSH |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| n .5827 +0.0007/-0.0000 is oversized on both holes .5838 & .5841 n .3543 ± 0.0004 is oversized on both holes .3552 - .3554 Surface finish 63 is over 120. ¦f¦.003¦A¦ measures 0.0093 Distance .261 ± 0.003 is oversized 0.2695 Inner Blended corner due to broken tool |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |