# MFD NON-COMPLIANCE REPORT # 6050

Date: 2/10/04

Job #:  18033, 18

Part Number:  pf-341-392-90

## Part Description:  Weld Adaptor

Engineer: Al Owens, x3168

Reason For Non-compliance:

- Dia. 3.978  +.000/-.002 is 3.976 – 3.980 – both parts

- Dia. 3.918 +.000/-.006 is 3.917 – 3.920 – both parts

Note:  See inspection report for details.

Action Taken:

Engineer Signature: __________________________