# MFD NON-COMPLIANCE REPORT # 7104

| PART NAME: | Wall “A” Support Plate 2 | DATE: | 10/12/05 |
| --- | --- | --- | --- |
| PF/SA NO.: | PF-380-708-49/0 | INSPECTOR: | T. Nakashima |
| WORK ORDER NO.: | 20443-28 | ENGINEER: | L. Eriksson | EXT.: | 3699 |
| VENDOR | MFD | ROUTE TO: | Welding |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| 1. 3.50 + - .020 is undersized by .080” 2. 45 degrees + - 30’ is undersized by 2 degrees, actual measurement is 43.5 degrees. |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |