# MFD NON-COMPLIANCE REPORT # 7116

| PART NAME: | Chamber Main Weldment | DATE: | 12/6/05 |
| --- | --- | --- | --- |
| PF/SA NO.: | SA-235-976-34 | INSPECTOR: | T. Nakashima |
| WORK ORDER NO.: | 20764-3 | ENGINEER: | D. Walz | EXT.: | 3270 |
| VENDOR | MFD | ROUTE TO: | Clean Weld |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| .930 + - .005 are undersized by .013” Actual measurement is .912” on part #1 are undersized by .015” Actual measurement is .910” on part #2 No on flatness of .010” on 1.110” face because of the welds on both parts. 3. Flatness of .010” exceeds by .002” on both parts. Actual flatness is .012” |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |