# MFD NON-COMPLIANCE REPORT # 7122

| PART NAME: | WG + CT SE2 F-MBJ ASSY | DATE: | 1/26-06 |
| --- | --- | --- | --- |
| PF/SA NO.: | SA-380-602-43 | INSPECTOR: | T. Nakashima |
| WORK ORDER NO.: | LCLS/LINAC | ENGINEER: | G. Diaz | EXT.: | 4184 |
| VENDOR | 20768-12 | ROUTE TO: | Precision Braze |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| #10 has braze material on the inside. #11 is -.100” on length of 17.88 +-.030, actual is 17.780 (-.070) #27 2.44 +-.030 is -.091”, actual is 2.349 (-.061) #28 2.44 +-.030 is -.060”, actual is 2.380 (-.030) |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |