# MFD NON-COMPLIANCE REPORT # 7156

| PART NAME: | RF Seal Finger 2 | DATE: | 5/1/06 |
| --- | --- | --- | --- |
| PF/SA NO.: | PF-451-060-92 | INSPECTOR: | T. Nakashima |
| WORK ORDER NO.: | 21196-18 | ENGINEER: | A. Ringwall | EXT.: | 8508 |
| VENDOR | MFD | ROUTE TO: | MTLFNSH |

| Reason For Non-Compliance: | Action (UAI,RWK,SCRP) |
| --- | --- |
| 2x Dia. .081” are oversized by .002” .178 + - .010 are oversized by .007” to .009” .240 +.020 -.000 are undersized by .001” to .004” |  |

| Engineer Signature: |  | Date: |  |
| --- | --- | --- | --- |