## Slide 1
engineering type: 0.788D11.5
SLAC drawing number: SA-237-005-02-R2
SLAC magnet bar-code: 4545
vendor serial number: N/A
when measured: 14-Feb-2018 16:28:55
when analyzed: 15-Feb-2018
MAD assignment: BCXDLU2

## Slide 2
quadrupole component
artificially removed
BCXDLU2: ΔBL/BL0 vs X @ 250 A
Imain | b1/b0 % | b2/b0 %
250.11 | 0.0333 | 0.2620
tolerance | 0.5 | 100
Harmonic content vs Imain @ r = 2 cm